NANO HIGHLIGHTS

Large Scale 3-D Directed Assembly of SWNTs and Nanoparticles
NSF NSEC Grant Number:   EEC-0425826

NSEC: Center for High-Rate Nanomanufacturing (CHN)

PI: A. Busnaina1, J. Mead2, G. Miller3, N. McGruer1 and C. Barry2
Northeastern Univ. 1, Univ. of Massachusetts Lowell2 and Univ. of New Hampshire3

The goal of this project is to develop a large scale low temperature template-less assembly technique to make a universal platform for integration of nanoelements into three dimensional architectures. This effort will directly help assembly goals of the CHN.  This universal 3D platform would find direct applications in 3D interconnects, 3D nano-electromechanical systems, 3D nanoelement sensors and for in-line characterization of manufactured nanomaterials.

We have successfully integrated SWNTs and Au nanoparticles into 3D interconnects and structures using a new alternative hybrid technique using dielectrophoresis. The concept of 3D interconnects has been demonstrated using the SWNT architectures.  A FEM simulation was carried out to predict the trajectory of these SWNTs during assembly.

Figure 3. Three-diemnsional Directed Assembly of

Gold Nanoparticles (2)

- Makaram, P., Selvarasah, P. Xiong, X.,  Chen, C., Busnaina, A., Khanduja, N., and Dokmeci, M., “Three-dimensional assembly of single-walled carbon nanotube interconnects using dielectrophoresis,” Journal of Nanotechnology cover and featured article, Volume 18, # 39, October 3,  2007.

- Xiong, X., Busnaina, A., Selvarasah, S., Somu,  S., Wei, M., Mead, J., Chen, C., Aceros, J.,  Makaram, P., and Dokmeci, M.,  “Directed assembly of gold nanoparticle nanowires and networks for nanodevices,” Appl. Phys. Lett.  91, 2007.

# Text boxes

200nm

Figure 2: I-V measurements of the 3D SWNT assembled at 10 at 10 Vp-p before and after encapsulation (1).

Figure 1: FESEM image of bundled SWNTs assembled between the top and bottom metal assembled at 5 Vp-p. (1)