NANO OVERVIEW

Design of Biocompatible Nanoparticles for Probing Living Cellular Functions 
and their Potential Environmental Impacts

NSF NIRT Grant BES 0507036

PIs:  X. Nancy Xu1, D. Gillet2, C. Osgood1, H. Elsayed-Ali1, R. Van Duyne3

1Old Dominion University, Norfolk, VA; 2CEA in France; 3Northwestern University

Research Activities and Findings:

In the second year of the NIRT project, we have accomplished an array of research and educational activities and achieved some of our proposed objectives, as outlined below:

Aim 1:  We have designed and prepared stable (non photodecomposed and non-aggregated) nanoparticles with controlled size and shapes for probing biocompatibility of nanoparticles and for the study of membrane transport of living bacterial cells in real-time, as showed in Fig. 1.1

Fig. 1:  Characterization of optical properties and stability of single Ag nanoparticles.

- Representative UV-vis absorption spectra of 0.71 nM Ag nanoparticles well-dispersed in egg water (1.2 mM) at 28˚C for (a) 0 and (b) 120 hours show that the peak absorbance and wavelength at 396 nm remain unchanged for 120 hours;

- Representative HR-TEM images of Ag nanoparticles show the size and spherical shape of single Ag nanoparticles.  Scale bar = 5 nm;

- Dark-field optical image of representative single Ag nanoparticles shows the majority of nanoparticles are blue with some being green and few are red;

- LSPR spectra (color) of representative single Ag nanoparticles exhibit peak wavelength at 452, 531, and 601 nm, respectively, showing size-dependent optics.

- LSPR spectra of representative single nanoparticle (a) before and (b) after irradiating by under dark-field microscope illuminator (100 W halogen) for 12 hr.  The illumination power at the sample stage (focal plane of dark field) is 0.070 ± 0.001 Watt.

- Representative plots of scattering intensity of (a) single nanoparticles and (b) background versus illumination time show that single Ag nanoparticles resist photobleaching and blinking.

Moreover, we have prepared nanoparticles that are stable in desired buffer solutions, egg water and cell culture media, allowing us to investigate the biocompatibility of the nanoparticles in living cells and in vivo model systems, and to probe the dependence of membrane transport upon the size, shape and surface properties of the nanoparticles.

We have also successfully synthesized and characterize functional Ag nanoparticles, and investigated the dependence of their optical properties, biocompatibility, and stability on the functional groups.  We have used these nanoparticles as single nanoparticle sensors to real-time image and detect single ligand-receptor interaction on single living cells.2

Our Co-PI (Van Duyne) at Northwestern University has focused on the optical and structural characterization of single nanoparticles of differing shapes and surface functionalization, as well as developing wide field imaging techniques for single-nanoparticle spectroscopy.3

Aim 2: We have been investigating the biocompatibility of nanoparticles, and are currently designing the fusion proteins, that will allow us to study how membrane proteins assemble the extrusion membrane transporter in response to a variety of nanoparticles.

Aim 3: We have studied the biocompatibility and cytotoxicity of Ag and Au nanoparticles.  We have begun to assess the potential impacts of these synthetic nanoaprticles on the environment using an in vivo model system, zebrafish embryos.

We found that individual Ag nanoparticles can passively diffuse into developing embryos via chorion pore canals, create specific effects on embryonic development and selectively generate particular phenotypes in a dose-dependent manner (Fig. 2), indicating the possibility of using nanoparticles as therapeutic agents.  The early embryos are highly sensitive to the nanoparticles, showing the possibility of using zebrafish embryos as an in vivo assay to screen the biocompatibility and toxicity of nanomaterials.3  This study represents the first direct observation of passive diffusion of nanoparticles into an in vivo system (an important aquatic species), suggesting that the release of large amounts of Ag nanoparticles into aquatic ecosystems (e.g., rivers) may have drastic environmental consequences, should the sizes of nanomaterials remain unchanged during environmental transport.

# Educational and Outreach Activities

- We have developed a new interdisciplinary course, entitled Frontiers in Nanoscience and Nanotechnology (Chem/Bio/ECE 460/560) for graduate and undergraduate students.  We are gathering teaching materials and plan to co-teach this course in the coming years.

- We have given several invited public seminars about this NIRT program around the nation.

- Our students have actively participated in Scholarship Day, Research Day and Chemistry week, at which our students gave a tour of our labs and performed several demo experiments to local high school students, and educated the general public about nanoscience, nanotechnology and this NIRT program.

In summary, this NIRT program allows us to engage an array of research and educational activities.  In this second year, we generated 9 publications, 5 invited chapters, 1 book, and gave over 10 invited presentations.  Our study has contributed to an array of disciplines, and has enhanced our collaborative activities and educational and research infrastructure of our university.

# References

1. K. Lee, P. Nallathamby, L. Browning, C. Osgood, X. Xu*, ACS Nano, 1, 133 (2007)

2. T. Huang, P. Nallathamby, D. Gillet, X. Xu*, Anal. Chemistry, 79, 7708 (2007)

3. E. Hicks, O. Lyandres, M. Glucksberg, and R. P. Van Duyne, J. Phys. Chem. C, 111, 4116 (2007).

4. For further information email: xhxu@odu.edu; visit website: http://www.odu.edu/sci/xu/nirt/nirt.html

# Text boxes

Fig. 2: Illustration of transport of single Ag nanoparticles into a cleavage stage zebrafish embryo, leading to normally developed, deformed and dead zebrafish.

B.

A.

C.

D.

F.

E.