NSF Nanoscale Science and Engineering Grantees Conference, Dec 3-6, 2007 Grant # : 0609140

NANO HIGHLIGHT
Utilization of Ballistic Deflection Phenomena for Room Temperature Devices
and Circuitry

NSF NIRT Grant 0609140

Marc Feldman, Martin Margala+, Paul Ampadu, Yonathan Shapir

University of Rochester, +University of Massachusetts Lowell

The Ballistic Deflection Transistor (BDT) is a novel device that is based upon an electron steering and a ballistic deflection effect.  Composed of an InGaAs-InAlAs heterostructure on an InP substrate, this material system provides a large mean free path and high mobility to support ballistic transport at room temperature.  The planar nature of the device enables a two step lithography process, as well, implies a very low capacitance design.   This transistor is unique in that no doping junction or barrier structure is employed.  Rather, the transistor utilizes a two-dimensional electron gas (2DEG) to achieve ballistic electron transport in a gated microstructure, combined with asymmetric geometrical deflection.  Motivated by reduced transit times, the structure can be operated such that current never stops flowing, but rather is only directed toward one of two output drain terminals.  Some of the unique properties of the BDT is that it possesses both a positive and negative transconductance region, enabling circuits that are inverting and non-inverting, depending only on gate offset voltage.  Experimental measurements have indicated that the transconductance of the device increases with applied drain-source voltage. DC measurements of prototype devices have verified small signal voltage gains of over 150, with transconductance values from 45 to 90 mS/mm depending upon geometry and bias.  Gate-channel separation is currently 80nm, and allows for higher transconductance through scaling. The six terminal device structure enables a normally differential mode of operation, and provides two drain outputs.  These outputs, depending on gate bias, are either complementary or non-complementary. This facilitates a wide variety of circuit design techniques.  Given the ultralow capacitive design, initial estimates of ft, for the device fabricated with a 430nm gate width, are over a THz.

Figure 1.  Pictured is a BDT with

430nm gates and 80nm gate-channel

Vdd spacing, the top-left and top right ports

are drain ports, bottom left and right

ports are gates, top port is a vdd bias

port that controls gain, and the bottom

L-drain R-drain port is the source. Dark regions

indicate etched material.

L-gate R-gate

Vss