NSF Nanoscale Science and Engineering Grantees Conference, Dec 3-6, 2007 Grant # : 0609087

Engineered Molecular Fluidics

NSF NIRT Grant 0609087

PIs: S.S. Sheiko1 , K. Matyjaszewski2, M. Rubinstein1 , O. Velev3 1University of NC at Chapel Hill, 2Carnegie Mellon University, 3North Carolina State University

Research Area and Objectives

Researchers are continuously looking for new flow systems and actuation principles that will allow molecular assays and synthesis to be performed on ever smaller scales.1,2 Our project explores a new direction in microfabricated fluidics – molecular fluidics wherein one can monitor, probe, and manipulate flows one molecule at a time (Fig. 1). With this intention, we study fluid monolayers that can be moved about by either external stimuli or by intrinsic means such as the interaction with the substrate. In addition to smaller volumes, monolayer systems also have advantages in direct accessibility, flow control, rapid heat exchange, and substrate involvement into mixing and orientation of macromolecules.

This research will advance fundamental understanding of the conformation and dynamics of surface-confined polymer chains and lead to the development of new theories for interfacial flow and its interaction with electric fields. Surfaces electrically controlled by “turning knobs” will lead to creation of a new range of materials and devices.  Since molecular conformation responds to flow and may respond to external stimuli such as electric fields, we anticipate the development of molecular sensors/triggers that can both probe and actively affect the flow properties. The molecular-scale understanding will also aid in lubrication of microscopic joints and microlithography. With this technology one should be able to fabricate surfaces that can have anisotropic wetting, directional liquid transport, and anisotropic tribology, and may even direct the growth of live cells for biomaterials and implants.

Methods employed

Our approach involves synthetic design of flow-responsive molecules, experimental and theoretical studies of surface-confined macromolecules under flow, and the engineering of flow actuation techniques. We have assembled an interdisciplinary team of leading scientists with respective experience in molecular visualization (Sheiko), polymer synthesis (Matyjaszewski), microfluidics (Velev), and theory & computer simulation (Rubinstein). A combination of optical, electrical, and scanning probe methods are applied to study the flow properties over a broad range of length scales from the motion of the film front all the way down to the movements of the individual molecules within the film.3,4 Experimental findings are tested against theoretical predictions and computer simulation studies, and also guide the polymer synthesis.

Molecular Pressure Sensors

Measurement of the flow of thin films is complicated by the coupling of frictional forces and the driving force (pressure gradient) at the molecular level. We designed a set of pressure-responsive molecular brushes with flexible side chains connected to a flexible backbone. When

NSF Nanoscale Science and Engineering Grantees Conference, Dec 3-6, 2007 Grant # : 0609087

the molecules are driven across a substrate, pressure-induced desorption of side groups causes the backbone to coil, and the extent of this compacting can be used to gauge local variations in film pressure.5,6 We tracked flow of the pressure-responsive macromolecules on both hydrophilic and hydrophobic substrates using atomic force microscopy (AFM) (Fig. 2). After appropriate calibration, these molecular pressure sensors give the friction coefficient at the substrate, which reveal strong humidity dependence on the hydrophilic mica substrate, though not on hydrophobic graphite (Fig. 2, table). The applicability range of the molecular pressure sensors was extended by mixing a small fraction of brush molecules with linear polymer melts of the same chemical composition (Fig. 2a). Fig. 2b demonstrates that the brushes (i) mix with their linear counterparts and (ii) respond to compression. The flow behavior of embedded macromolecules was tested against theoretical predictions within static monolayers7 and compared to conformational changes under different environmental conditions.8

Flow-enhanced molecular diffusion and ordering

Long-range orientational order in monolayers of brush-like macromolecules was achieved during flow of a polymer monolayer on the surface of highly oriented pyrolytic graphite. The domain size varied from ca. 1 to 10 µm which is noticeably larger than the submicrometer-sized mosaic blocks typically observed upon adsorption from solution. The increase in the degree of order is attributed to the flow-enhanced diffusion of the macromolecules within spreading monolayers which facilitates the epitaxial alignment of the large macromolecules. The diffusion coefficient was shown to increase linearly with the spreading rate. Even though the ordering occurred during flow, no correlation was observed between the molecular orientation and the flow direction (Fig. 3). Thus, the role of the flow was not to induce the molecular orientation but

to facilitate the intrinsic ordering process. These findings can inspire and lead to new strategies for constructing large scale ordered structures on

Figure 3. Flow-induced molecular ordering. High magnification images on graphite reveal no correlation

surfaces. In a similar way,

flow-induced diffusion of

between the flow direction and

molecules within dense

orientation of the flowing molecules.

monolayers is expected to 
enhance mixing, fractionation,9 and reactions of flowing molecules.

NSF Nanoscale Science and Engineering Grantees Conference, Dec 3-6, 2007 Grant # : 0609087

Molecular electrowetting and electroconvective crystallization

We discovered and began characterizing a new electroosmotic effect in aqueous films of nanoscale thickness. The films are spontaneously formed on hydrophilic mica surfaces and are sustained at a thickness on the order of tens of nanometers by the intrinsic disjoining pressure. We found that the liquid inside these films begins to move intensively when subjected to tangential DC electric fields on the order of 50 V/cm. This can be explained on the basis of electroosmotic motion of the dense counterionic layer near the charged mica surface. This finding will give us the ability to study and control the liquid flow on the nanoscale and investigate the flows of ionic solutions in ultrathin films with a free interface. We demonstrated that the flow velocity is linear with regards to the intensity of the driving electric field as predicted by the general theory of electroosmosis. Methods for precise measurement of the liquid velocity profile are being explored presently. We are developing devices for molecular electrowetting where the liquid flow will be laterally restricted by a pattern on the substrate.

We also demonstrated that electrowetting on partially hydrophobic surfaces can be conveniently controlled by addition of surfactant. Another new phenomenon related to the electrowetting effect that we observed was the formation of particle chains near the three-phase contact line during the application of electric field and a resulting long-range alignment of the 2D crystal that is deposited during the film drying. This finding might provide a convenient method for long-range colloidal crystallization during the deposition of particulate films from withdrawing meniscus Figure 4. Electroosmotic manipulation of

with suspension. molecular fluorophore in an ultrathin film.

References

For further information about this project contact  sergei@email.unc.edu

[1] Reyes, D. R.; Iossifidis, D.; Auroux, P. A.; Manz , A. "Micro total analysis systems. Introduction, theory, and technology. " Anal. Chem., 74, 2623-2636 (2002).

[2] Stone, H. A.; Stroock, A. D.; Ajdari, A. "Engineering flows in small devices: Microfluidics toward a lab-on-achip." Ann. Rev. Fluid Mech. 36, 381-402 (2004).

[3] Xu, H.; Shirvaniants, D.; Beers, K.; Matyjaszewski, K.; Rubinstein, M.; Sheiko, S.S. "Molecular Motion in a Spreading Precursor Film." Phys. Rev. Lett. 93,  206103, (2004).

[4] Xu, H.; Sheiko, S.S.; Shirvaniants, D.; Rubinstein, M.; Beers, K.L.; Matyjaszewski, K.; “Flow induced epitaxial ordering of brush-like macromolecules on graphite” Langmuir 22, 1254-1259 (2006).

[5] Xu, H.; Shirvaniants, D.; Rubinstein, M.; Shabratov, D.; Beers, K.; Matyjaszewski, K.; Sheiko, S.S. “Molecular Pressure Sensors” Advanced Materials 19, 2930-2934 (2007).

[6] Editors’ Choice, “A Measured Flow” Science 318, 535 (2007).

[7] Sun, F.C.; Dobrynin, A.V.; Shirvanyants, D.; Lee H.-I., Matyjaszewski, K.; Rubinstein, G.; Rubinstein, M.; and Sheiko, S.S. “A Flory Theorem for Structurally Asymmetric Mixtures“  Phys. Rev. Lett. 99, 137801 (2007).

[8] Gallyamov, M.O. et al. “Vapour-induced Spreading Dynamics of Adsorbed Linear and Brush-like Macromolecules as Observed by Environmental-SFM” Journal of Polymer Science B, 45, 2368-2379 (2007).

[9] Barrett, M., Sun, F.C., Sheiko, S.S. J. Am. Chem. Soc. (to be submitted).