# Nanotube-array based lithography

NSF NER, Grant #0609349

PI: Punit Kohli

Department of Chemistry and Biochemistry

Southern Illinois University

Carbondale IL 62901

Students: Pradeep Ramiah Rajasekaran, Justin Wolff, Rashid Zakeri, Bojan Mitrovic, Charvi Patel and Kashyap Tadinisa.

Collaborators: Sami Aouadi (Department of Physics) and Haibo Wang (Department of Electrical Engineering) Southern Illinois University;  Horacio Espinosa (Department of Mechanical Engineering) Northwestern University; Christina Trautmann (GSI, Germany)

Nano-lithography has proven to be one of the leading approaches for a controllable patterning of molecules at nano- and micro-scale levels. Though many other methods for patterning molecules and nanoparticles at the nanoscale are currently available, they have some limitations such as high throughput rate, simultaneously patterning of different molecules, and relatively expensive instrumentation.  Here we show a novel method for fabricating a conical pore in a glass matrix (called chip) which was used to pattern a FITC-tagged DNA onto a gold coated substrate using electrophoretic transport mechanism.  The fabricated chips were mounted on a home-made 3-D piezoelectric motors for demonstration of patterning of nucleic acids.  Our deposition system may find many potential applications from  patterning semiconductors to performing reactions at molecular level.

Figure 1. Schematic of Instrumentation              Figure 2.  Schematic of Pen with DNA writing

# Figure 3. Different types of DNA patterns formed on substrates with the application of positive potential. Top figure shows that patterning does not occur  when negative potential is applied and occurs only when positive potential is applied.

References:

- Ho, Andrea M.; Rim, Jee; Kohli, Punit; Patankar, Neelesh; Espinosa, Horacio D. “Electric-field Induced Direct Delivery of Proteins by a Nanofountain Probe”  PNAS. 2008. 105. 16438-16443.

- Pradeep, Ramiah Rajasekaran; Wolff, J.; Zakeri, R.; Mitrovic, B.; AouadiS.; Trautmann,C.; Kohli, P. “Lithography using Nanotubes”, JACS (in preparation).

- Mirkin, C. et al. Science, 1999, 283, 661-663.

Acknowledgement. The authors would like to thank NSF (CMMI) for funding this work through grant  #0609349.